INFORMATION FOR DIGITAL PRINTING ON 100% COTTON VELOUR TOWELS

1] Digital printing is the printing using computer technology. Since this is Digital Printing we can print with almost 100% Accuracy from the Original Design. The machine COLARIS 3 used for Printing is from J.Zimmer  Maschinenbau, GmBH, Austria, which uses state of the art technology for printing on cotton towels.

2] It obsoletes older printing technology which have a lot of design and colour constraints

3] Today's digital printing is performed using the CMYK ink. These colours can be combined to get all the pantone shades.

4] The use of ink assists us in bringing out the colour Brilliancy & Color Fastness of

Printing.

5] Ink & Chemicals required in the process are being imported from USA & Germany to give lustre, fastness & a soft feel.

6]     Designs for printing should be according to the points given below

- Designs should be in Tiff or JPEG format.

- Design should have High resolution (minimum 4K recommended)

- Designs should ideally have the same size & aspect ratio as that of the final product.

- Designs look better if they have sharp edges

- Designs should have extended backgrounds as the corners of the designs are printed on salvage. (3-5 cm on width & 5-7 cm on length, each side)

7]   The Digital Technology makes for very sharp and fine prints. Very Intricate designs

can be printed apart from this with almost 100% accuracy.

8]    Our machine we can print upto 185 cms width. Length is not an issue.

9]   We will require an order of atleast 1.5 to 2 tons in weaving for any particular given

SIZE & GSM.  We need a minimum of 380 gsm and can print upto 500 gsm and the

Number of designs can be upto 500 pcs per design or lesser. Our standard size is 75 x 150 cm and we can do lower quantities in the above size

10]  We use 2/24 Combed Yarn on the Pile which give a very soft feel and excellent Print

Clarity. Also please note the water which we use is R.O. for processing has a TDS less

than 50 ppm for ultimate softness and a good feel.